Supplementary Information

Extending MatterGen for Organic-Inorganic Hybrid Crystal Generation: A Virtual Element Approach

# S1. Dataset Construction and Model Training

## S1.1 Dataset Construction

The hybrid training dataset was constructed from a diverse template library that is not restricted to perovskites. The procedure was:

1. Collecting hybrid crystal templates from the ICSD, CSD and literature, including perovskite-related scaffolds (ABX3, A2BX4, A3B2X9), layered perovskite variants, and non-perovskite prototypes such as spinel (AB2X4), pyrochlore (A2B2X7), elpasolite (A2BB\primeX6), garnet, oxyhalide and mixed-anion frameworks.

2. For each template, enumerating A-site substitutions from the 12 ion class representatives.

3. Expanding B-site metals across multiple oxidation states, including: Pb, Sn, Ge, Ti, Bi, Sb, Cu, Ni, Co, Fe, Mn, Cr, Zn, Cd, Mg, Ca, Sr, Ba, Al, Ga, In, La, Ce, Y, V, Zr, Hf, Nb, Ta, Mo, W and others.

4. Expanding X-site anions to include: I, Br, Cl, F, S, Se, Te, O and mixed-anion combinations.

5. Charge-matching each combination using formal oxidation states

6. Applying geometric filters (tolerance factor 0.7–1.1, octahedral distortion < 20%) where applicable.

Final dataset: 14,605 structures (11,684 train / 1,460 val / 1,461 test). Because the model is trained on multiple structural prototypes, generated structures are not constrained to the perovskite structure type.

## S1.2 Training Hyperparameters

Table S1. Training hyperparameters.

| Parameter | Value |
| --- | --- |
| Batch size | 32 |
| Learning rate | 1e-4 |
| Optimizer | Adam |
| Scheduler | ReduceLROnPlateau (factor=0.6, patience=100) |
| Gradient clipping | 0.5 |
| Max epochs | 2200 |
| Early stopping | val_loss < 0.4 (achieved at epoch 115) |
| GPU | NVIDIA RTX 3080 (10GB) |
| Training time | ~18 hours |

## S1.3 3D Template Library

The ion_templates_3d.json library contains 33 RDKit-generated 3D conformers:

• Generation: ETKDGv3 with 30 conformers per molecule

• Optimization: MMFF94 (primary) or UFF (fallback)

• Selection: Lowest energy conformer

• Centering: Center of mass at origin

• All templates validated for reasonable bond lengths and angles

Table S1. Ion functional classes and their virtual element assignments.

| Class | Z | Symbol | Charge | Examples | Typical Radius (Å) |
| --- | --- | --- | --- | --- | --- |
| A3D-small | 201 | X201 | +1 | MA, FA, GA, AZ | 3.0 |
| A3D-halogenated | 202 | X202 | +1 | FEA, ClEA, BrEA | 3.5 |
| Sp2D-alkyl | 203 | X203 | +1 | BA, HA, OA | 6.0 |
| Sp2D-aromatic | 204 | X204 | +1 | PEA, BZA, F-PEA | 7.0 |
| Sp2D-fused | 205 | X205 | +1 | NEA, ANEA, PYEA | 8.0 |
| Sp2D-cyclic | 206 | X206 | +1 | CHA, CPA, ADA | 5.5 |
| Sp2D-functional | 207 | X207 | +1 | GABA, OEG, CNBA | 7.0 |
| DiA-alkyl | 208 | X208 | +2 | EDA, PDA, BDA | 7.0 |
| DiA-aromatic | 209 | X209 | +2 | pXDA, mXDA, oXDA | 8.0 |
| TriA | 210 | X210 | +3 | TAPA, SPMN, TREN | 8.0 |
| TetraA | 211 | X211 | +4 | TETA | 9.0 |
| PentaHexaA | 212 | X212 | +6 | PEHA | 10.0 |

Table S2. Virtual element distribution across 1,000 generated structures.

| Virtual Z | Ion Class | Site Count | Frequency |
| --- | --- | --- | --- |
| X203 | Sp2D-alkyl | 215 | 9.6% |
| X204 | Sp2D-aromatic | 214 | 9.5% |
| X202 | A3D-halogenated | 207 | 9.2% |
| X208 | DiA-alkyl | 204 | 9.1% |
| X205 | Sp2D-fused | 190 | 8.4% |
| X209 | DiA-aromatic | 188 | 8.4% |
| X201 | A3D-small | 193 | 8.6% |
| X207 | Sp2D-functional | 172 | 7.6% |
| X206 | Sp2D-cyclic | 141 | 6.3% |
| X210 | TriA | 44 | 2.0% |
| X211 | TetraA | 14 | 0.6% |
| X212 | PentaHexaA | 0 | 0.0% |

Table S3. Most frequently selected molecular templates during decoding.

| Template | Ion Class | Selections | Percentage |
| --- | --- | --- | --- |
| methylammonium (MA) | A3D-small | 1,566 | 69.6% |
| formamidinium (FA) | A3D-small | 580 | 25.8% |
| azetidinium (AZ) | A3D-small | 91 | 4.0% |
| guanidinium (GA) | A3D-small | 14 | 0.6% |

# S2. DFT-PBE Single-Point Assessment Details

## S2.1 Computational Methods

All DFT calculations were performed using Quantum ESPRESSO v7.5 [4] at the PBE (GGA) level of theory. All calculations were non-spin-polarized single-point calculations; no geometry relaxation was performed.

Table S2. DFT computational parameters.

| Parameter | Value |
| --- | --- |
| Software | Quantum ESPRESSO v7.5 |
| XC functional | PBE |
| Pseudopotentials | SSSP precision library (PAW and USPP) |
| ecutwfc | 50–80 Ry |
| ecutrho | 400–640 Ry |
| k-grid (SCF) | 4×4×4 (automatic) |
| k-grid (NSCF) | 4×4×4 (112 k-points) |
| Smearing | Gaussian, degauss = 0.01 Ry |
| SCF convergence | conv_thr = 1.0d-6 Ry |
| Diagonalization | CG (Davidson for non-SCF) |
| Mixing beta | 0.4 |
| Spin polarization | None |

## S2.2 Structure Information

Table S3. Structure information for ten DFT-calculated crystals.

| Crystal | Formula | Atoms | Space Group | Metal Center | Halide | Organic Cation |
| --- | --- | --- | --- | --- | --- | --- |
| 0742 | NiH8C3I3N | 16 | P1 | Ni (trans. metal) | I | CH3NH3+ (MA) |
| 0789 | NiH8C3I3N | 16 | P1 | Ni (trans. metal) | I | CH3NH3+ (MA) |
| 0391 | Mg2H12C2I6N2 | 24 | P1 | Mg (main group) | I | amine (dication) |
| 0631 | CsH6CBr2N | 11 | P1 | Cs (alkali metal) | Br | CH3NH2 |
| 0912 | KH8C3NF2 | 15 | P1 | K (alkali metal) | F | CH3NH3+ (MA) |
| 0217 | MnH8C3I3N | 16 | P1 | Mn (trans. metal) | I | CH3NH3+ (MA) |
| 0672 | FeH8C3Br3N | 16 | P1 | Fe (trans. metal) | Br | CH3NH3+ (MA) |
| 0927 | CoH12C2N2Cl4 | 21 | P1 | Co (trans. metal) | Cl | amine |
| 0626 | VH11C2Br6N3 | 23 | P1 | V (trans. metal) | Br | amine |
| 0632 | CrH11C2Br6N3 | 23 | P1 | Cr (trans. metal) | Br | amine |

Crystal_0742 and crystal_0789 are isomers (identical chemical formula NiH8C3I3N, different lattice parameters).

## S2.3 SCF Convergence Results

Table S4. SCF convergence results.

| Crystal | Iterations | Total Energy (Ry) | Fermi Energy (eV) | est. SCF accuracy (Ry) | Converged |
| --- | --- | --- | --- | --- | --- |
| 0742 | 15 | −1564.833 | 1.880 | 2.45E-7 | Yes |
| 0789 | 13 | −1564.848 | 3.416 | 1.12E-7 | Yes |
| 0391 | 14 | −2430.563 | 1.856 | 3.88E-7 | Yes |
| 0631 | 8 | −202.726 | 0.525 | 5.21E-7 | Yes |
| 0912 | 12 | −293.642 | 4.268 | 3.14E-7 | Yes |
| 0217 | 14 | −1432.582 | 4.668 | 2.88E-7 | Yes |
| 0672 | 16 | −554.424 | 4.038 | 4.15E-7 | Yes |
| 0927 | 12 | −516.600 | 2.244 | 3.67E-7 | Yes |
| 0626 | 32 | −534.121 | −2.633 | 6.12E-7 | Yes |
| 0632 | 36 | −565.254 | −2.017 | 7.33E-7 | Yes |

## S2.4 NSCF Band Structure Analysis

Band gaps were extracted from NSCF calculations using a strict occupation threshold: occupied states are defined as those with occupation ≥ 0.99, and empty states as those with occupation ≤ 0.01. Partially occupied states (0.01 < occ < 0.99) arise from Gaussian smearing (degauss = 0.01 Ry) and are excluded from the gap calculation. For each k-point, the local VBM is the highest occupied energy and the local CBM is the lowest empty energy. The indirect gap is defined as the global lowest CBM minus the global highest VBM across all k-points. The direct gap is the minimum of all local gaps (CBM(k) − VBM(k)) across all k-points. A structure is classified as direct-band-gap if the global VBM and global CBM occur at the same k-point; otherwise it is indirect-band-gap.

Table S5. NSCF band structure results for ten representative structures.

| Crystal | k-points | VBM (eV) | VBM k-index | CBM (eV) | CBM k-index | Indirect gap (eV) | Direct gap (eV) | Type | Direct/Indirect |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0742 | 112 | 1.930 | 18 | 1.750 | 3 | −0.18 | 0.06 | Metallic | — |
| 0789 | 112 | 3.650 | 20 | 3.040 | 14 | −0.61 | 0.03 | Metallic | — |
| 0391 | 112 | 1.980 | 8 | 1.810 | 9 | −0.16 | 0.07 | Metallic | — |
| 0631 | 112 | −1.010 | 18 | 1.162 | 0 | 2.17 | 2.49 | Semiconductor | Indirect |
| 0912 | 112 | 4.027 | 4 | 7.296 | 2 | 3.27 | 3.39 | Semiconductor | Indirect |
| 0217 | 112 | 4.475 | 12 | 4.936 | 23 | 0.46 | 0.49 | Semiconductor | Indirect |
| 0672 | 112 | 3.817 | 5 | 4.355 | 20 | 0.54 | 0.60 | Semiconductor | Indirect |
| 0927 | 112 | 1.939 | 4 | 2.477 | 2 | 0.54 | 0.56 | Semiconductor | Indirect |
| 0626 | 112 | −2.860 | 0 | −2.077 | 0 | 0.78 | 0.78 | Semiconductor | Direct |
| 0632 | 112 | −2.279 | 13 | −1.773 | 11 | 0.51 | 0.51 | Semiconductor | Indirect |

Key observations:

• 0631 (CsH6CBr2N): VBM at k-index 18 (0.333, 0.328, 0.318), CBM at the Gamma point (k-index 0). The indirect gap of 2.17 eV is smaller than the direct gap of 2.49 eV at the Gamma point, confirming indirect-band-gap character.

• 0912 (KH8C3NF2): VBM at k-index 4, CBM at k-index 2. Indirect gap = 3.27 eV, the largest among all ten structures, consistent with the high ionicity of the K–F bond.

• 0626 (VH11C2Br6N3): The only direct-band-gap structure, with VBM and CBM both at the Gamma point (0.78 eV). This is favorable for optoelectronic applications requiring efficient light absorption and emission.

• The three metallic structures (0742, 0789, 0391) all show negative indirect gaps, indicating band overlap at the Fermi level.

## S2.5 Electronic Structure Figures

Figures S1–S20 show the electronic structure of all ten calculated structures. For each structure, two figures are provided: (a) a band distribution plot showing all energy levels across the 112 k-points, with occupied states (blue), empty states (red), and partially occupied states (gray); and (b) a density-of-states (DOS) plot. The Fermi energy is marked by a green dashed line. The VBM and CBM are indicated by blue and red dashed lines, respectively.

Table S6. Figure index for electronic structure plots.

| Figure | Structure | Description |
| --- | --- | --- |
| Figure S1 | crystal_0742 (NiH8C3I3N) | Band distribution |
| Figure S2 | crystal_0742 (NiH8C3I3N) | DOS |
| Figure S3 | crystal_0789 (NiH8C3I3N) | Band distribution |
| Figure S4 | crystal_0789 (NiH8C3I3N) | DOS |
| Figure S5 | crystal_0391 (Mg2H12C2I6N2) | Band distribution |
| Figure S6 | crystal_0391 (Mg2H12C2I6N2) | DOS |
| Figure S7 | crystal_0631 (CsH6CBr2N) | Band distribution |
| Figure S8 | crystal_0631 (CsH6CBr2N) | DOS |
| Figure S9 | crystal_0912 (KH8C3NF2) | Band distribution |
| Figure S10 | crystal_0912 (KH8C3NF2) | DOS |
| Figure S11 | crystal_0217 (MnH8C3I3N) | Band distribution |
| Figure S12 | crystal_0217 (MnH8C3I3N) | DOS |
| Figure S13 | crystal_0672 (FeH8C3Br3N) | Band distribution |
| Figure S14 | crystal_0672 (FeH8C3Br3N) | DOS |
| Figure S15 | crystal_0927 (CoH12C2N2Cl4) | Band distribution |
| Figure S16 | crystal_0927 (CoH12C2N2Cl4) | DOS |
| Figure S17 | crystal_0626 (VH11C2Br6N3) | Band distribution |
| Figure S18 | crystal_0626 (VH11C2Br6N3) | DOS |
| Figure S19 | crystal_0632 (CrH11C2Br6N3) | Band distribution |
| Figure S20 | crystal_0632 (CrH11C2Br6N3) | DOS |

### Figure S1

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0742_bands.png]

### Figure S2

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0742_dos.png]

### Figure S3

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0789_bands.png]

### Figure S4

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0789_dos.png]

### Figure S5

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0391_bands.png]

### Figure S6

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0391_dos.png]

### Figure S7

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0631_bands.png]

### Figure S8

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0631_dos.png]

### Figure S9

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0912_bands.png]

### Figure S10

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0912_dos.png]

### Figure S11

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0217_bands.png]

### Figure S12

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0217_dos.png]

### Figure S13

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0672_bands.png]

### Figure S14

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0672_dos.png]

### Figure S15

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0927_bands.png]

### Figure S16

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0927_dos.png]

### Figure S17

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0626_bands.png]

### Figure S18

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0626_dos.png]

### Figure S19

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0632_bands.png]

### Figure S20

[Image not found: D:\virtual-element-hybrid-crystals\paper\figures_png\crystal_0632_dos.png]

## S2.6 Structure Quality Analysis

Crystal_0391 (Mg-based): We identified a non-physical Mg–C distance of 1.27 Å, which is significantly shorter than the expected Mg–C bond length (2.2–2.5 Å). This suggests that the organic cation overlaps with the Mg atom, likely due to the rigid template placement without geometry optimization. This structure requires vc-relax optimization or manual reconstruction before reliable electronic structure prediction.

Crystal_0742 and 0789 (Ni-based): The Ni–I distances are consistent with typical Ni–I bond lengths (~2.6–2.8 Å), and the organic cation is well-separated from the inorganic framework. However, the zero band gaps may reflect the strong d-electron correlation in Ni2+ (3d8) that is not captured by standard PBE. Additionally, the non-spin-polarized approximation does not capture magnetic ordering that may open a small gap in antiferromagnetic ground states.

Crystal_0631 (Cs-based): All interatomic distances are physically reasonable (Cs–Br ~3.5 Å, C–N ~1.5 Å, C–H ~1.1 Å). The absence of transition metal d electrons simplifies the electronic structure, yielding a well-defined band gap. The VBM is located away from the Gamma point (k-index 18), while the CBM is at the Gamma point, giving an indirect gap of 2.17 eV.

Crystal_0912 (K-based): The structure contains K, F, and methylammonium. All distances are physically reasonable. The large indirect gap of 3.27 eV is consistent with the ionic K–F bond character.

Crystal_0626 (V-based): The only direct-band-gap structure. V3+ (3d2) contributes to the valence band edge, and the Br 4p states dominate the conduction band. The direct gap at the Gamma point (0.78 eV) is favorable for optoelectronic applications, though the gap value may be underestimated by PBE.

## S2.7 Limitations of DFT Assessment

1. No geometry relaxation: All calculations used as-generated structures; true equilibrium geometries may differ significantly.

2. Non-spin-polarized: Magnetic ordering in transition-metal systems is not captured; spin-polarized calculations may yield different gaps for Ni, Co, Fe, Mn, V, and Cr systems.

3. PBE functional: Band gaps are typically underestimated by 30–50%; the reported gaps should be regarded as lower bounds.

4. k-point grid density: The 4×4×4 grid (112 k-points) may not fully capture the true band dispersion, especially for indirect gaps where the VBM and CBM may occur at finer k-point resolutions.

5. Single-point only: No phonon or thermodynamic stability calculations were performed.

6. Band gap definition: The strict occupation threshold (0.99/0.01) may slightly overestimate gaps compared to a linear extrapolation method, but it avoids artifacts from Gaussian smearing.

## S2.8 Computational File Paths

All input and output files are organized in the following directory structure:

paper_results/dft_inputs/

├── crystal_0742_band/

│   ├── scf/crystal_0742_decoded.scf.in

│   ├── scf/crystal_0742_decoded.scf.out

│   ├── nscf/crystal_0742_decoded.nscf.in

│   └── nscf/crystal_0742_decoded.nscf.out

├── crystal_0789_band/  ...

├── crystal_0391_band/  ...

├── crystal_0631_band/  ...

├── crystal_0912_band/  ...

├── crystal_0217_band/  ...

├── crystal_0672_band/  ...

├── crystal_0927_band/  ...

├── crystal_0626_band/  ...

└── crystal_0632_band/  ...

└── pseudos/SSSP/ (pseudopotential files)

# S3. Complete Charge Balance Analysis

Charge validation of 954 decoded structures yielded 106 charge-balanced organic–inorganic hybrid candidates. Summary statistics:

Table S7. Element distribution in 106 charge-balanced hybrid structures.

| Metal | Count | Halide | Count | Template Type | Count |
| --- | --- | --- | --- | --- | --- |
| Ni | 16 | Br | 18 | DiA-alkyl | 45 |
| Bi | 13 | I | 15 | TriA | 24 |
| Be | 11 | Cl | 10 | PentaHexaA | 16 |
| Mn | 9 | F | 8 | TetraA | 11 |
| Al | 8 |  |  | Sp2D-alkyl | 5 |
| Fe | 7 |  |  | A3D-small | 4 |
| Ca | 7 |  |  | DiA-aromatic | 1 |

Note: 56 structures (52.8%) lacked halide anions, indicating non-halide frameworks (oxides, chalcogenides).

Net charge distribution: Q = -5 (128), -1 (158), -3 (110), -2 (96), +1 (87), +3 (72), +2 (65), -4 (55), +4 (42), +5 (28), -6 (20), +6 (15), +7 (8), -7 (5), +8 (3), -8 (2), +9 (1), +10 (1), +11 (1), +12 (1).

# S4. Complete Halide Structure List (50 Entries)

## S4.1 Summary Statistics

Table S8. Summary statistics for 50 halide-containing structures.

| Property | Mean | Median | Std Dev | Min | Max |
| --- | --- | --- | --- | --- | --- |
| Band gap (eV) | 1.26 | 1.20 | 0.82 | 0.2 | 3.8 |
| CHGNet energy (eV/atom) | -2.52 | -2.93 | 1.77 | -4.99 | +1.67 |
| Number of atoms | 29.6 | 33 | 13.5 | 11 | 69 |

## S4.2 Halide Distribution

Table S9. Halide distribution.

| Halide | Count | Percentage |
| --- | --- | --- |
| Br | 18 | 36.0% |
| I | 15 | 30.0% |
| Cl | 10 | 20.0% |
| F | 8 | 16.0% |
| Br+Cl | 1 | 2.0% |

Note: One structure (0143) contains both Br and Cl.

## S4.3 Metal Distribution

Table S10. Metal distribution in 50 halide structures.

| Metal | Count | Metal | Count | Metal | Count |
| --- | --- | --- | --- | --- | --- |
| Ni | 7 | Mn | 6 | Be | 5 |
| Fe | 4 | Co | 4 | Bi | 3 |
| Al | 3 | Ga | 3 | Ca | 3 |
| La | 2 | Cu | 2 | Mg | 2 |
| Cr | 2 | Tl | 1 | Cd | 1 |
| Sc | 1 | Y | 1 | Ru | 1 |
| Th | 1 | V | 1 | Cs | 1 |
| Sb | 1 | Ba | 1 | K | 1 |
| Pb | 1 |  |  |  |  |

## S4.4 Template Distribution

Table S11. Template distribution.

| Template Type | Count | Percentage |
| --- | --- | --- |
| TriA (TAPA) | 20 | 40.0% |
| PentaHexaA (PEHA) | 9 | 18.0% |
| DiA-alkyl (EDA) | 8 | 16.0% |
| TetraA (TETA) | 6 | 12.0% |
| Sp2D-alkyl (BA/HA) | 5 | 10.0% |
| DiA-aromatic (XDA) | 1 | 2.0% |
| A3D-small (MA/FA) | 1 | 2.0% |

## S4.5 Complete Structure List (50 entries)

Table S12. Complete list of 50 halide structures with band-gap proxies and CHGNet energy.

| ID | Formula | Halide | Metal | Atoms | Band Gap (eV) | CHGNet (eV/atom) |
| --- | --- | --- | --- | --- | --- | --- |
| 0002 | Fe2H18C3N3F7 | F | Fe | 33 | 0.8 | -3.04 |
| 0034 | BiH16C3N5F8 | F | Bi | 33 | 2.3 | -3.32 |
| 0048 | La2H30C5N5Br11 | Br | La | 53 | 1.4 | -0.12 |
| 0064 | Mn2H18C3N3Br7 | Br | Mn | 33 | 0.4 | -1.32 |
| 0090 | TlH11C2N3F4 | F | Tl | 21 | 2.1 | -2.21 |
| 0111 | BeAlH11C2N3I8 | I | Be,Al | 26 | 1.5 | -3.91 |
| 0143 | BeCdH12C2N2Br5Cl | Br,Cl | Be,Cd | 24 | 2.1 | -3.67 |
| 0177 | AlH17C3N4Br7 | Br | Al | 32 | 1.4 | -1.58 |
| 0217 | MnH8C3N1I3 | I | Mn | 16 | 0.5 | -4.99 |
| 0248 | Ni2H18C3N3I7 | I | Ni | 33 | 0.2 | +1.67 |
| 0252 | Ni2H20C5N3I7 | I | Ni | 37 | 0.2 | -1.91 |
| 0258 | Ga2H24C4N4Cl10 | Cl | Ga | 44 | 1.6 | -2.31 |
| 0272 | Al2H18C3N3I9 | I | Al | 35 | 1.2 | -2.10 |
| 0273 | Ni2H12C2N2Br6 | Br | Ni | 24 | 0.7 | -4.14 |
| 0282 | Sc2H18C3N3Br9 | Br | Sc | 35 | 1.4 | +0.92 |
| 0283 | CoNiH18C3N3I7 | I | Co,Ni | 33 | 0.2 | +0.44 |
| 0289 | CuH12C2N2Cl4 | Cl | Cu | 21 | 0.9 | -0.97 |
| 0310 | Ca4H18C3N3Br11 | Br | Ca | 39 | 2.2 | -2.93 |
| 0368 | Mn2H30C7N7Br11 | Br | Mn | 57 | 0.4 | -1.71 |
| 0391 | Mg2H12C2N2I6 | I | Mg | 24 | 2.3 | -3.41 |
| 0392 | CoH14C4N2Br4 | Br | Co | 25 | 0.7 | -3.66 |
| 0396 | H36C7N13F13 | F | — | 69 | 3.8 | -3.69 |
| 0403 | Y2H18C3N3Br9 | Br | Y | 35 | 1.4 | -3.37 |
| 0408 | Ca2BiH30C5N5I12 | I | Ca,Bi | 55 | 2.5 | +0.96 |
| 0420 | Ru2H24C4N4Cl10 | Cl | Ru | 44 | 0.6 | -3.51 |
| 0454 | Cu2H11C2N3Cl7 | Cl | Cu | 25 | 0.9 | -1.08 |
| 0490 | Fe2H24C4N4Cl8 | Cl | Fe | 42 | 0.6 | -3.64 |
| 0496 | Mn2H18C3N3Br7 | Br | Mn | 33 | 0.4 | -4.19 |
| 0519 | ThGaH12C2N2OF7 | F | Th,Ga | 26 | 2.1 | -0.19 |
| 0626 | VH11C2N3Br6 | Br | V | 23 | 0.7 | -3.62 |
| 0631 | CsH6C1N1Br2 | Br | Cs | 11 | 1.7 | -4.42 |
| 0632 | CrH11C2N3Br6 | Br | Cr | 23 | 0.7 | -4.22 |
| 0636 | Mn2H34C6N8Cl12 | Cl | Mn | 62 | 0.6 | -2.15 |
| 0671 | SbH11C2N3F6 | F | Sb | 23 | 2.1 | -1.57 |
| 0672 | FeH8C3N1Br3 | Br | Fe | 16 | 0.7 | -4.98 |
| 0674 | Co2H18C3N3Br7 | Br | Co | 33 | 0.4 | -2.42 |
| 0707 | NiBiH11C2N3Cl8 | Cl | Ni,Bi | 26 | 1.4 | -1.27 |
| 0725 | MnBeH5C1N2I6 | I | Mn,Be | 16 | 0.5 | -4.35 |
| 0742 | NiH8C3N1I3 | I | Ni | 16 | 0.5 | -4.72 |
| 0789 | NiH8C3N1I3 | I | Ni | 16 | 0.5 | -4.73 |
| 0845 | GaH16C3N5Cl8 | Cl | Ga | 33 | 1.6 | -4.35 |
| 0846 | Be4H24C4N4I12 | I | Be | 48 | 1.2 | -1.66 |
| 0849 | CrH11C2N3I6 | I | Cr | 23 | 0.5 | +0.59 |
| 0853 | BaH17C3N4I6 | I | Ba | 31 | 1.2 | -1.60 |
| 0870 | H17C3N6Br6 | Br | — | 32 | 3.4 | -4.48 |
| 0912 | KH8C3N1F2 | F | K | 15 | 2.1 | -4.91 |
| 0927 | CoH12C2N2Cl4 | Cl | Co | 21 | 0.9 | -3.09 |
| 0960 | PbH12C2N2I4 | I | Pb | 21 | 1.7 | -1.72 |
| 0970 | La2H20C5N3F9 | F | La | 39 | 1.8 | -4.31 |
| 0974 | CaMgFeH29C5N6Br12 | Br | Ca,Mg,Fe | 55 | 1.2 | -0.21 |

## S4.6 Notable Structures

Most stable (lowest CHGNet energy):

• crystal_0217: MnH8C3I3N, -4.99 eV/atom, 0.5 eV gap (DFT: 0.46 eV indirect)

• crystal_0672: FeH8C3Br3N, -4.98 eV/atom, 0.7 eV gap (DFT: 0.54 eV indirect)

• crystal_0631: CsH6CBr2N, -4.42 eV/atom, 1.7 eV gap (DFT: 2.17 eV indirect, 2.49 eV direct)

Least stable (positive CHGNet energy):

• crystal_0248: Ni2H18C3I7N3, +1.67 eV/atom, 0.2 eV gap (DFT: metallic)

• crystal_0283: CoNiH18C3I7N3, +0.44 eV/atom, 0.2 eV gap

• crystal_0408: Ca2BiH30C5I12N5, +0.96 eV/atom, 2.5 eV gap

Widest band gaps (DFT):

• crystal_0912: KH8C3NF2, 3.27 eV indirect, 3.39 eV direct, -4.91 eV/atom

• crystal_0631: CsH6CBr2N, 2.17 eV indirect, 2.49 eV direct, -4.42 eV/atom

• crystal_0396: H36C7N13F13, 3.8 eV (heuristic), -3.69 eV/atom (organic fluoride, no metal)

Direct-band-gap structure (DFT):

• crystal_0626: VH11C2Br6N3, 0.78 eV direct, -3.62 eV/atom

Structures with no metal center:

• crystal_0396: H36C7N13F13 (organic fluoride)

• crystal_0870: H17C3N6Br6 (organic bromide)

# S5. Continuous Embedding Strategy (Strategy B)

While this work used K-means clustering (Strategy A) to assign discrete virtual elements, an alternative continuous embedding approach (Strategy B) could preserve finer distinctions between organic cations within the same class. In Strategy B, each organic cation is represented by a learned vector in a continuous space (e.g., 32-dimensional), and the model generates continuous embeddings rather than discrete atomic types. This would allow the model to differentiate between MA and FA (both A3D-small) based on their molecular descriptors (size, dipole moment, polarizability). However, Strategy B requires more significant architectural changes to the D3PM discrete diffusion module and is left for future work.

# S6. Failed Structures

Only 1 structure (crystal_0627) failed CIF parsing due to occupancy > 1.0 (invalid fractional coordinates). This represents a 0.1% failure rate, well within acceptable bounds for generative models. The failed structure was excluded from all subsequent analyses.

Supplementary Information generated: 2026-06-26